# Text boxes

Photos are showing the “Medico 5” model (front/back)

Salten Skovvej 2, DK-8653  Them, Denmark

Phone: +45 86 84 73 66

Fax: +45 86 84 80 77

E-mail: ct@ct-mail.dk

Internet: www.combi-therm.dk

Combi-Therm 3-layer Thermal carrierbag

Specifications:

| Item No…………. | : | Medico 5 |
| --- | --- | --- |
| Print……………... | : | Standard is without any print |
| Size……………... | : | W 400mm x H 410/50mm + 50mm flap |
| Outerfoil………… | : | 55 micron silver pe |
| Insulation……….. | : | 70 gr/m² polyester fibers |
| Innerfoil…………. | : | 55 micron silver pe |
| Handle/closing…. | : | Tape closing/sealing –system |
| Carton…………… | : | 75 pcs. - size 59x39x31cm |
| Pallet……………. | : | 24 crts. - EUR 80x120x207cm |

The 3-layer quality thermal bags from Combi-Therm/Cot products A/S are made of strong high-tech and lightweighted thermal material, produced in Denmark and exported all over the world. During the years the 3-layer thermal bags continuosly have been improved, offering the best possible thermal bag solution. A quality thermal bag consist of min. 3 layers of which one layer is made of insulation material (PE foam or polyester fibers).The 3-layer thermal carrier bags from Combi-Therm/Cot products A/S are produced of PE with respect for the environment, are food safe (FDA and BGA approved) and can be recycled.